5
The purpose of using SE for internal combustion engine components is to provide
wear protection whilst at the same time maintaining a low-friction coefficient (µ<0.1)
in an oil-lubricated operating environment. Typically, piston rings, cam-followers
(valve lifters), cams, journal bearings and exhaust valves (Fig. 8.1) receive dedicated
surface modification via a variety of techniques.

7
There are few oil-lubricated sliding contacts more important than the piston ring/
cylinder liner contact found in petrol- and diesel-fired internal combustion (IC)
engines. Typically three or four piston rings are used in a collection of rings on piston, termed the ‘ring pack’ (Fig. 8.1). Whilst the lower-positioned rings slide on
an oil film, providing a seal from combustion gases, the uppermost one – the ‘top
ring’ – enjoys less-efficient lubrication and is periodically exposed to hot combustion
gases as well as atmospheric oxygen. Furthermore, a range of lubrication regimes is
experienced by the piston ring/cylinder liner contact (Fig. 8.2), which depends upon
the position of the piston in the combustion cycle of the engine. Accordingly, the oil
fluid film periodically breaks down when the piston ring pack reaches bottom or top
dead centre in the combustion cycle; it is here where material transfer due to scuffing
(material transfer due to metal-on-metal or coating-on-metal contact), as well as
oxidation, can take place. During normal sliding between the top and bottom dead-
centre positions, however, boundary, mixed and full-film (EHL and HL) conditions
are established (Fig. 8.2) where only slight (if any) inter-material contact takes place.
In the latter situations, wear of the piston ring or the cylinder (or its liner) are
minimal.

8
Piston ring materials have evolved over the decades, originally being made of
flake graphitic cast iron (like GA-iron – Fig. 8.3a), which then became superseded by
the more fracture-resistant spheroidal graphitic cast iron (like SG-iron – Fig. 8.3b).
Both types of cast iron can be strengthened further via a heat treatment known as
‘hardening and tempering’, which converts the pearlitic matrix to fracture-resistant
‘tempered martensite’ – comprising fine-grained (~1µm) ductile alpha-iron (ferrite)
and very fine cementite (Fe3C) particles (1µm and smaller). For more demanding
applications, martensitic stainless steels are deployed, a typical nominal composition
being (wt-%): 0.9C, 18Cr, 0.1V and 1.1Mo. The high concentration of Cr provides protection against oxida-
tion attack from hot combustion gases, by the spontaneous formation of passive films
or scales based on chromium oxide (either crystalline Cr2O3 or amorphous CrxOy).
Such stainless steel rings are hardened and tempered to develop static and fatigue strength and are usually plasma or gas nitrided

11
Manufacturers began the SE of piston rings in the early part of the twentieth
century by applying many variants of electroplated Cr (Section 4.3.1) with various
crack densities and surface finishes (AE Goetze, 1995), mainly as a protective coat-
ing for cast iron substrates; these provide good protection against oxidation wear and
reduce scuffing/galling (metal transfer to the cast iron cylinder liner). The cracks
(Fig. 8.4a, b) help prevent scoring of the opposing liner by collecting wear debris and
retaining small pockets of oil lubricant. Under normal operating conditions, the
engine liner or cylinder wall is worn only slightly by superficial plastic flow (Fig. 8.4c)
and should not usually require any special surface treatment. Unfortunately, elec-
troplated Cr, or the alternative flame-sprayed Mo, whilst widely used on petrol
engine piston rings, is less satisfactory for diesel engine use.

12

By the mid 1980s,
a wide range of alternative metal, metal-ceramic (composite) and all-ceramic spray-
deposited coating materials (mostly deposited on cast iron substrates) had been
developed and implemented into mass production for diesel engine operation;
these were designed for use in small, medium and heavy-duty engines (Table 8.1).
Hence, the first three variants shown in the table are Mo matrix based and best serve
petrol-fired engines; they display very good scuffing resistance, with limited oxidation protection and micro-abrasion resistance. The plasma-sprayed MKP 81A
and MKP 107 ‘cermet’ coating systems (based on Mo-MoxCy or Mo-CrxCy –
Table 8.1) were designed for diesel engine use, where higher-temperature and more-
abrasive conditions exist. More recently, circa 2010, more-advanced versions of this
concept have been made (e.g., see MKJet 502 in Table 8.1), where a composition
within the WC-Cr3C2-Ni system has been developed for diesel engine use (Fig. 8.5).
These are applied using HVOF (see Chapter 4, Section 4.14.6) technology and are
reputed to have a higher cohesive strength and better bonding to their cast iron
substrate compared to the aforementioned plasma-spray variants. Unfortunately,
the HVOF process is relatively expensive, and its conversion efficiency from powder
particles to a functional coating is quite low – in some cases, more than 60% of the
spray powder can be lost as ‘over-spray’. Such factors provide a large impetus for the
development of new coating technologies and new coating materials for use in mass
production.

13
For very abrasive engine situations, ‘all-ceramic’ plasma spray coatings like the
Al2O3-TiO2 (KP123) composition (Table 8.1) perform better than the previously
mentioned cermet compositions. Here, abrasion resistance is provided by the Al2O3
phase, whilst the TiO2 constituent helps augment fracture toughness and maintain
low friction (µ<0.1), simultaneously restricting scuffing/galling. However, attempts
to augment this idea further by developing coatings consisting almost entirely of Ti
sub-oxide (TiOx) or TiO2 (Landa et al, 2005) have not been entirely successful.

During the late 1980s, a novel hybrid coating technology was created to produce
a new high-durability coating at low production cost. Here, hard aluminium oxide
(Al2O3) particles were incorporated into a chromium plating This coating material was
implemented into mass production during the 1990s; it remains in use today.
The precise details of the process are proprietary, but it is reliant on varying the
polarity of the substrate from positive to negative during growth of the Cr plating.
Interruption of the deposition phase by relatively short cycle durations of applied
positive polarity exaggerates the formation of cracks through electro-etching (as in
Fig. 8.4a). At this juncture in the process, fine (~0.5 to 15µm) particles of Al2O3,
suspended in the liquid electrolyte become concentrated into the Cr plating cracks
(possibly via an electrophoretic action); the polarity is then returned to its initial
cathodic character, and Cr deposition is resumed, so as to enclose the particles within
the Cr matrix of the coating.

16
Valve lifter (cam-follower) and cam shaft materials have not received very much
change in the past thirty years. The review of Becker (2004) indicates no changes in
the principal materials used for these devices when compared to those highlighted in
publications during the 1980s (Eyre & Crawley, 1980; Eyre, 1984). The summary
given in Table 8.3 is still relevant at the time of writing (circa 2015); this shows a high
reliance on cast irons and steels for valve lifters and cams. Here, surface engineering
is required to realise a combination of high fatigue endurance, fatigue strength,
rolling contact fatigue (RCF) pitting resistance, micro-abrasion wear and scuffing
(material transfer) resistance. Scuffing is minimised by the phosphating (with man-
ganese phosphate) of steel or cast iron valve lifters or by using micro-cracked Cr
electroplating (similar to that shown in Fig. 8.4a). The latter procedures enable oil
retention and spreading, which greatly aid boundary lubrication. Formulated oils
containing anti-wear additives, like ZDDP (Bec et al, 1999; Barnes et al, 2001;
Spikes, 2004; de Barros Bouchet et al, 2005), although widely used to aid an anti-
scuffing character, can also initiate premature rolling contact fatigue pitting (Eyre &
Crawley, 1980). Adverse pinholing of DLC coatings (presently being introduced for
valve lifter applications) may also be triggered by oil additives (Section 8.3.3).